## Slide 1
2
29
YR3-ePDF Analysis
Each distance has 0.275 microns approximately
29 analysis points
from
surface to 8 micron deep
OBSIDIAN SURFACE
Only the first Si-O 1.6 Å, 2.4 Å ?, O- O 2.7 Å and Si-Si 3.2 Å distances are distinguishable in all SiO2 polymorphs

## Slide 2
First Peak position (red line) Stay in the sample Place
Second Peak position (blue line) have small systematic shift once we go from 2 to 29
YR3-ePDF Analysis from 29 different locations
Only the first Si-O 1.6 Å, 2.4 Å ?, O- O 2.7 Å and Si-Si 3.2 Å distances are distinguishable in all SiO2 polymorphs
Si-O 1.6 Å
O- O 2.7 Å

## Slide 3
Height of the first Peak (red arrow) drops once we go from 2 to 29
Height of the second peak (green arrow) increases once we go from 2 to 29
Height of the third Peak (blue arrow) increases once we go from 2 to 29
YR3-ePDF Analysis
Si-O
?
O-O
Coordination number variation of Si-O, O-O, Si-Si PDF peaks are roughly equivalent to their peak height ; this varies with distance from surface, reveals possible true variation of hydration layer from surface of the sample
Only the first Si-O 1.6 Å, 2.4 Å ?, O- O 2.7 Å and Si-Si 3.2 Å distances are distinguishable in all SiO2 polymorphs

## Slide 4
Chart: YR_3_11Aout2020 / ePDF peaks height / 1sec exp time
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24

peak 1 | 1.5 | 1.475 | 1.39 | 0.987 | 0.815 | 0.472 | 0.565 | 0.402 | 0.474 | 0.342 | 0.388 | 0.253 | 0.275 | 0.177 | 0.207 | 0.13 | 0.148 | 0.097 | 0.128 | 0.078 | 0.076 | 0.13 | 0.127 | 0.142

peak 2 | 0.293 | 0.284 | 0.272 | 0.198 | 0.167 | 0.0925 | 0.111 | 0.077 | 0.091 | 0.064 | 0.075 | 0.049 | 0.052 | 0.0375 | 0.041 | 0.03 | 0.031 | 0.026 | 0.029 | 0.027 | 0.039 | 0.057 | 0.072 | 0.034
Chart: YR_3_11Aout2020 / ePDF peaks height / 2sec exp time
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24

peak 1 | 1.382 | 1.46 | 1.214 | 1.084 | 0.786 | 0.537 | 0.536 | 0.458 | 0.45 | 0.398 | 0.366 | 0.292 | 0.265 | 0.206 | 0.198 | 0.147 | 0.141 | 0.117 | 0.123 | 0.095 | 0.101 | 0.069 | 0.068 | 0.044

peak 2 | 0.288 | 0.301 | 0.439 | 0.238 | 0.174 | 0.114 | 0.113 | 0.095 | 0.092 | 0.081 | 0.074 | 0.058 | 0.052 | 0.042 | 0.039 | 0.033 | 0.03 | 0.029 | 0.029 | 0.027 | 0.027 | 0.026 | 0.025 | 0.026
e-PDF Peak height evolution (coordination number) with depth
Si-O coordination number
O-O coordination number
Si-O coordination number
Si-Si coordination number
Coordination number variation of Si-O with distance from surface, reveals possible true variation of hydration layer from surface of the sample
Only the first Si-O 1.6 Å, 2.4 Å ?, O- O 2.7 Å and Si-Si 3.2 Å distances are distinguishable in all SiO2 polymorphs
Each distance has 0.275 microns approximately

## Slide 5
Chart: YR_3_11Aout2020 / ePDF peaks height / 2sec exp time
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24

peak 1 | 1.382 | 1.46 | 1.214 | 1.084 | 0.786 | 0.537 | 0.536 | 0.458 | 0.45 | 0.398 | 0.366 | 0.292 | 0.265 | 0.206 | 0.198 | 0.147 | 0.141 | 0.117 | 0.123 | 0.095 | 0.101 | 0.069 | 0.068 | 0.044

peak 2 | 0.288 | 0.301 | 0.439 | 0.238 | 0.174 | 0.114 | 0.113 | 0.095 | 0.092 | 0.081 | 0.074 | 0.058 | 0.052 | 0.042 | 0.039 | 0.033 | 0.03 | 0.029 | 0.029 | 0.027 | 0.027 | 0.026 | 0.025 | 0.026
Number 6 : 1,65 m
Number 15 : 4,12 m
Number 13: 3.57 m
First inflection point (red arrow at 1,65 m)
Saturation layer ?
End hydration layer (blue arrow)
blue arrow 4,12 m
12.000 YEARS OF HISTORY ?